G270… HOT AIR BLOWER

Tube: Black, smooth, EPDM rubber compounded for maximum heat resistance.
Reinforcement: Double steel helix wire embedded between plies of spiralled textile cords.
Cover: Black, heat and weather resistant EPDM rubber with white stripe.
Temperature Range: -40°C (-40°F) to 150°C (302°F). Intermittent service to 175°C (347°F).