G922… POLY-AIR®
Tube: Black, high molecular-weight, medium oil-resistant PVC compound.
Reinforcement: High-tensile spiralled polyester yarn with longitudinal cords to give added strength and reduce elongation.
Cover: Smooth, red, abrasion and weather resistant, high molecular-weight PVC compound.
Temperature Range: -25°C (-13°F) to 65°C (149°F).